## Slide 1: Fibra Óptica
Notes: Fiber optic systems consist of light sources, transmission medium (cable, air), and some form of light detector. The concept of using light as a communications application was originally explored by Alexander Graham Bell. In the late 1800’s he experimented with a transmission device that he called the photophone. His system used sunlight and mirrors to transmit an audio signal. Even though he had some success in sending a signal over a short distance, he determined that this method was not practical for mass applications as the quality was very poor.

## Slide 2: Enlace Óptico Típico
E/O
O/E
Emendas
DIO´s
Conectores
ópticos
E = Electrônico
O = Óptico
Notes: Transmitter:
    Converts Data Signal to Light Pulses
    Uses Light Emitting diode (LED) or Laser Diode (LD)
Receiver:
    Converts Light Pulses to Data Signal
    Uses Photo Diode Detector (PIN or APD)
Distribution Cabinet:
    Terminates Outside Cable Sheath
    Separates Individual Fibers for Coupling to Transmitter and Receiver
    Allows for Patching and Splicing of Fibers
Connector:
    Connects Optical Fibers at Transmitter, Receiver and Patch Panels.
Splice:
    Can be Mechanical or Fusion
Optical Cable:
    Carries Optical Modes from Source to Receiver.

## Slide 3: Experimento Básico sobre Guiamento da Luz
Luz
Tubo de água
Luz guiada
Notes: One of the early experiments conducted on guided light was performed in the mid nineteenth century by an Irish scientist named John Tyndall.
Creating a stream of water from a bucket with a hole near the bottom, he used a mirror to guide sunlight into the stream. Once the light entered the stream, it followed the curved path of the water stream.
The created some interest but did not prove to be very useful. It did demonstrate the refraction of light.

## Slide 4: Energia Electromagnética
Ultra
Violeta
Violeta
Azul
Verde
Amarelo
Laranja
Vermelho
Infraverm.
400
455
490
550
580
620
750
800
850
Luz visível
1022
1021
1020
1019
1018
1017
1016
1015
1014
1013
1012
1011
1010
109
108
107
106
Ultravioleta
Raios-X
Infravermelho
Radar
TV & FM Radio
Raios Gamma
Raios Cósmicos
Freqüência
1 THz
1 GHz
1 MHz
Radio Ondas Curtas
Radio AM
Comprimento
de onda em nm
Espectro Eletromagnético
Notes: The lightwave spectrum covers the range from ultraviolet through visible light and infrared. Lightwaves are electromagnetic energy and behave according to the same laws as microwaves.
Glass is the primary material of lightwave waveguides. The glass materials used for the optical waveguides (fibers) exhibit decreasing loss with an increase in wavelength.
The first fiber optic systems operated in the short wavelength region because light sources and detectors were readily available.

## Slide 5: Comprimento de onda (Wavelength)
Pico-a-Pico
Amplitude
Wavelength
Um Ciclo
Freqüência = 4 Ciclos por segundo (4 Hz)
1 Segundo
Notes: <number>
<footer>
<header>
<date/time>
Wavelength of Light - Since light is an electromagnetic wave it has the same characteristics as any other wave (amplitude, frequency, and phase). Wavelength is measured in meters and is the distance that one cycle of the light signal travels. The wavelength is dependent upon the frequency of the variation and its velocity of transmission ( = velocity/frequency).
In the electromagnetic spectrum optical radiation lies between microwaves and x-rays. It is common to use wavelength rather than frequency when dealing with high-frequency electromagnetic waves such as light. In fiber optics, wavelength is important because it can be measured directly. The wavelength of light is typically measured in nanometers (nm), micrometers (m), and angstroms (A), instead of feet or inches. Nanometers is the unit most often used with fiber optics. One nanometer is 10e-9m, and 1 angstrom is 10e-10m, therefore, 1 nanometer is equal to 10 angstroms.
Visible light includes all wavelengths between 10 nm and 1 mm. Within this range are ultraviolet, visible light and infrared radiation. Visible light is defined as radiation that stimulates the sense of sight, that is, affects our optic nerve. It includes all radiation from 390 to 770 nm, from violet to red. Light itself does not have color, but these wavelengths stimulate color receptors in the eye. The visible spectrum is just a small fraction of the electromagnetic spectrum. A typical wavelength used in fiber optics is 850 nm, which may be expressed as 0.850 m, or 8500A. This wavelegth is designated as infrared.

## Slide 6: Largura de Linha Espectral
800
900
Intensidade
Comprimento de onda (nm)
LED
Laser
Notes: Any light source emits light with its own:
    Set of colors
    or
    Range of wavelengths
Optical fiber transmitters for glass optical fibers normally emit light at, or near, one of the three following nominal wavelengths measured in nanometers (nm).
    850 nm
    1300 nm
    1550 nm
    This nominal value is called the center wavelength

## Slide 7: Largura Espectral Usual
Intensidade
Máxima
Meia
intensidade
(FWHM)
Intensidade
Comprimento de onda
Notes: The total power emitted by a transmitter is distributed over a range of wavelengths spread around the center wavelength. This range is the spectral width. Spectral width is measured in nanometers.
Spectral widths vary from narrow (several nanometers) to wide (from tens to hundreds of nanometers) depending on the type of source used. Wide spectral widths lead to increased dispersion of light pulses as the light pulses propagate through a fiber.
Note: Spectral width (or pulse width) is usually given as the range of wavelengths emitted with an intensity level greater than, or equal to, one-half of the peak intensity level or Full Width Half Maximum (FWHM) spectral width.

## Slide 8: Interferência Electrostática
Receiver
Dados com Erros
Receiver
Dados sem Erros
Cobre
Fibra
Notes: RFI
Copper cable transmission systems transmit signals by the flow of electrons through the copper conductor. Electrostatic interference, such as lightning, can alter the flow of those electrons causing errors in the received data signal.
Fiber optic systems transmit signals by the flow of photons or lightwaves through the fiber. Photons are not effected by electrostatic interference and the system will therefore operate error free.
EMP
Fiber Optic cable is not totally immune from Electro Magnetic Pulses (Radiation). Fiber optic cables exhibit great resistance to EMP. Radiation effects will discolor standard fiber types; however, laser based systems do clear up some of the degradation after a period of time. Special optical fibers can be purchased for usage in application where EMP is a concern.

## Slide 9: Interferência Electromagnética
Receiver
Dados com Erros
Receiver
Dados sem Erros
Cobre
Fibra
Power Line
Notes: As in the case with electrostatic interference, fiber optic systems are also immune to electromagnetic interference whereas copper systems are not. As the magnetic lines of flux expand around the power line the reach the copper and fiber optic conductors. As the flux lines cut across the copper they induce a small electric current that interferes with the signal being conducted in the copper cable.
Fiber systems are also unaffected by differences in ground potentials at the two ends of the system. The performance of copper systems, on the other hand, can be adversely affected by differences in ground potentials between the terminal equipment. In some installations, this may mean special precautions in grounding and expensive isolation transformers must be employed to ensure reliable and safe operation.

## Slide 10: Luz no Material
Velocidade = c
Velocidade v < c
n = 1
n > 1
Índice de Refração n = c/v
Notes: Electromagnetic energy, such as light, travels at approximately 300,000 meters per second (186,000 miles per second) in free space (C).
C = 300,000 Kilometers/Sec = 3 x 108 M/Sec
For propagation in free space and in the atmosphere, the speed of light is the same for all wavelengths. In other materials, such as water and glass, different wavelengths travel at different speeds. Regardless of the wavelength, when light travels through materials, its speed is noticeable reduced. Bacause of this, a light ray moving from air into a solid or a liquid will change direction at the surface of the new medium which is know as refraction. In optics, a medium is any substance that transmits light.
In materials more dense than free space (such as glass), the velocity of electromagnetic waves is reduced (the speed of light is decreased). When this reduction in velocity takes place, the light ray is refracted toward the normal when it passes from one medium to another medium of a denser material. The normal is simply a line drawn perpendicular to the interface at the point where the incident ray strikes the interface. When a light ray enters a less dense material, the ray bends away from the normal.
The speed, V, when divided into the speed of light in a vacuum, C, yields the Index of Refraction, N.

## Slide 11: Impedância do Vidro
n1 = 1
Z2
Vidro
Z1
n2 = 1.5
R
(4%)
Notes: The Impedance (Zn), of Glass is:
Zn = Zo/n Where Zo is the impedance of a vacuum
and is = to 377
4% of the light energy at the interface is reflected back, this occurs whether it is an air to glass or a glass to air transition. This results in a light power loss of 0.18 dB. This phenomenon is called Fresnel Reflection.
The reflection factor is:
n1
-
n2
n1
+
n2
2
r =

## Slide 12: Refração
Fonte de
Luz
Branca
Normal
Feixe não
refratado
Red
Orange
Yellow
Green
Blue
Violet
Vidro (Mais Denso)
AR
AR
Notes: Refraction: The bending of a beam of light in transmission between two dissimilar materials or in a graded index fiber whrere the refractive index is a continuous function of position.
Index of Refraction: The index of refraction is the ratio of light velocity in a vacuum compared to its velocity in the transmission medium. Light travels in a vacuum through space at 186,291 miles per second. Divided by it speed through optical glass (12,642 miles per second) the calculation for its index of refraction is 1.471.
A light ray (mode) is refracted as it passes from a material of a given density into a material of a different density. The light ray is not bent as previously believed, it changes direction at the interface. The refractive index of a material is wavelength dependent.
The example shows how sunlight, which contains all light frequencies, is affected as it passes through a material more dense than free space. Refraction occurs at both air/glass interfaces. Since colors of light are different frequencies and have different wavelengths, they are refracted differently. For visible light, the violet wavelengths are refracted the most, and the red wavelengths are refracted the least. The color separation of which light in this manner is called prismatic refraction. This phenomenon explains rainbows; water droplets in the atmosphere acting like small prisms that split the white sunlight into the various wavelengths creating a visible spectrum of color.

## Slide 13: Refração da Luz
n1 = 1
(vácuo)
n2 > 1 (mais denso)
(normal)
Notes: When light transitions from a media of one index of refraction to another media with a different index of refraction, and at an oblique (< 900) angle, the path of the light will be changed.
The light can be thought of as a series of wave fronts moving through a media. When these wave fronts encounter a more dense media, their speed decreases.
When they enter this media at an oblique angle, one end of the wave enters the denser media first, slowing down before the other end of the wave enters. This changes the direction of the wave toward the normal (perpendicular). If the light were traveling in the other direction, it would change direction away from the normal line.
There are two variables that effect refraction:
    Wavelength: Different colors travel at different speeds. Refractive index varies directly with wavelength. This effect may be seen though the use of prisms (red refracts less than violet).
    Temperature: Same color in same material travels at different speeds dependent upon temperature. Refractive index varies indirectly with temperature. This effect may be seen through mirages of the twinkling of stars.

## Slide 14: Reflexão Interna Total
Ar
Água
Notes: When light travels from a material of higher refractive index (more dense) to one of lower refractive index (less dense) it changes direction away from the perpendicular (normal). If the angle of incidence is too large, refraction occurs in a way that it either just skims the surface or does not enter the other material.

## Slide 15: Lei de Snell
sin A1 V1 n2
sin A2 V2 n1
=
=
A1
A2
n2
n1 > n2
Raio Escapa
A1
A2 = 900
n2
n1 = n2
Raio é Absorvido
A1
A2
n2
Reflexão Interna Total
n1
n1
n1
n1 > n2
Notes: Snell’s Law:
The ratio of the sine of the angle of incidence (A1) to the sine of the angle of refraction (A2) is equal to the ratio of the propagation velocities (V) of the wave in the two respective media. This is equal to a constant (K) which is the ratio of the refractive index of the second medium to that of the first (n2/n1). .

## Slide 16: Ângulo Crítico
Normal (N)
Ar
1.0
Vidro
1.5
Ângulo
Crítico
Reflexão
Refração
Notes: The critical angle is defined as the minimum angle of incidence at which a light ray may strike the interface of two media and result in an angle of refraction of 90 degrees or greater. (This definition pertains only when the light ray is traveling from a more dense medium into a less dense medium.) If the angle of refraction is 90 degrees or greater, the light ray is not allowed to penetrate the less dense material. Total reflection takes place at the interface, and the angle of reflection is equal to the angle of incidence.
The amount of refraction that occurs at the interface of two materials of different densities is quite predictable and depends on the refractive index of the two materials. The refractive index is simply the relation of the velocity of propagation of light in free space to the velocity of propagation of light in a given material. Mathematically, the refractive index is speed of light in free space (vacuum) divided by the speed of light in the material.
When light rays enter the fiber, they strike the air/glass interface at the normal. The refractive index of air is 1 and the refractive index of the glass core is 1.5. The light entering at the air/glass interface propagates from a less dense medium into a more dense medium. The light rays will refract toward the normal. This causes the light rays to change direction and propagate diagonally down the core at an angle which is different than the external angle of incidence at the air/glass interface. In order for a ray of light to propagate down the cable, it must strike the internal core/cladding interface at an angle that is greater than the critical angle

## Slide 17: Ângulo Crítico
c
c
n1
n2
Critical Angle c = Total Internal Reflection
1
1
n1
n2
2
n2 < n1
n1 sen c = n2sen90 = n2
Notes: At the interface of two transparent media’s with different indexes of refraction (n), light traveling in the higher density media (high value n) will be partially reflected and partially refracted by the media interface when an angle 1 is small.
As angle 1 increases, the angle of the refracted ray 2 increases until it equals 900, beyond this point, the critical angle, there is total internal reflection.

## Slide 18: Ângulo Crítico
n = 1.003
n = 1.33
N
I
N = Normal
I = Incidence
Critical
Angle
Notes: The path of a ray of light (mode) in different materials is influenced by the fact that light travels more slowly in an optically dense medium than it does in a less dense one. A measure of this effect is the refractive index.
A ray approaching an interface (boundary) between media of different refractive indices (e.g., glass-air) at an angle 0 to the normal in the higher index side, leaves at a greater angle o in the lower index medium.
A significant feature of refraction is that a small proportion of the light is reflected back into the originating medium (partial internal reflection)
At a particular value of the incident angle 0c, the refracted ray emerges parallel to the interface. This is identified as the critical angle. Any ray striking the interface at an angle greater than the critical angle will be reflected back into the medium (Total Internal Reflection).

## Slide 19: Núcleo, Casca e Revestimento (Core, Cladding, and Coating)
Revestimento
primário
Núcleo
Casca
Notes: <number>
<footer>
<header>
<date/time>
Fiber size is a measure of the core diameter and cladding (outside) diameter. It is expressed in a xx/zz format, where the xx is the core diameter and the zz is the outside diameter of the cladding. a 62.5/125 micron fiber would have a core diameter of 62.5 microns and a total diameter of 125 microns.
Core - The core of the fiber is made of exceptionally pure glass or plastic.
Cladding - The cladding is made of glass with a different refractive index than the core and is responsible for maintaining the light pulses within the core. The cladding also provides protection for the core.
Modal dispersion is the tendency of light to travel in a wavelike motion, rather than in a straight line. The greater the level of wave fluctuations, the greater the dispersion of the signal ad the associated degradation of performance.

## Slide 20: Índices de Refração na F.O.
Cabo Óptico
Casca n2
Núcleo n1> n2
Casca n2
(mais denso) n1 > n2 (menos denso)
Notes: The refractive index of a medium: The ratio of the velocity of light in a vacuum to the velocity of light in the medium. Light travels in a vacuum through space at 186,291 miles per second, and through optical glass at 126,642 miles per second.
n = C / Cm
Where C is the speed of light in a vacuum and Cm is the speed of light in the medium.
Typical indices of refraction are:
    Vacuum 1.0000
    Air 1.0003
    Water 1.33
    Quartz 1.46
    Glass 1.50
    Diamond 2.00
    Silicon 3.40

## Slide 21: Abertura Numérica (NA) (Numerical Aperture)
n0 = 1
NA
Núcleo n1 = 1.48
Ângulo Crítico c = sen-1 n2 / n1
Casca n2 = 1.46
c
Abertura Numérica NA = sen NA
NA = sen-1 NA
Notes: The ability to couple light into or out of a fiber is represented in its numerical aperture (NA). The NA of a fiber is the measure of the maximum angle (NA) of light entering the end of the fiber that will be propagated within the core of that fiber. NA is a figure of merit that is used to measure the light gathering or light collecting ability of an optical fiber.
Light rays entering the fiber that exceed this angle (NA) will exceed the critical angle (c) within the fiber and therefore will not be reflected back into the fiber’s core. These rays enter the fiber’s cladding and become cladding modes, which are eventually lost.
The Numerical Aperture (NA) is a function of the indexes of refraction of the core and the cladding of the fiber. A high NA fiber will accept light at a greater angle from the axis.

## Slide 22: Cone de Aceitação
Ângulo de Aceitação
Cladding Mode
NA
CL
Núcleo
Vista Tridimensional do Cone de Aceitação
Notes: The NA of a fiber defines the “Acceptance Cone”. Any light ray falling within the acceptance cone (angle) will be propagated within the fiber’s core by total internal reflection.
Light rays exceeding the acceptance angle will become cladding modes. Cladding modes will escape from the fiber over a relatively short distance.
The smaller the NA, the smaller the cone of acceptance and the more difficult it is to couple light into the fiber.
The half angle of the acceptance cone is designated as NA. As the numerical aperture (NA) increases, the angle of the acceptance cone increases. A large NA, which produces a larger acceptance cone, allows a greater amount of light to be coupled into the fiber.
A typical NA for Multimode fiber is 0.2, which gives a cone half angle of 11.5 degrees.

## Slide 23: Cone de Aceitação
Ângulo de
Aceitação
Cladding Mode
Fonte Óptica
Fibra
Notes: The optical source of light energy typically is considerably larger than the core of the fiber and produces light in a relatively wide cone. This causes the fiber to be overfilled (light enters not only the core but also the cladding).
Many (thousands) of rays (modes) of light will propagate down the core. There will also be many modes in the cladding that will escape over a relatively short distance.

## Slide 24: Efeitos de NA
Alto NA
Baixo NA
Notes: The variation is the Numerical Aperture (NA) effects the modal dispersion of the fiber. With a large NA, more modes (rays) of light enter the fiber and are transition through the fiber to the output. The arrival of the modes at the output of the fiber at different time intervals spreads the signal (modal dispersion).

## Slide 25: Características Físicas
62.5/125
50/125
100/140
9/125
Multimodo
Índice gradual
Multimodo
Índice gradual
Multimodo
Índice Degrau
Monomodo
Degrau
Núcleo / Casca
Notes: <number>
<footer>
<header>
<date/time>
Multimode fiber was the first commercially available type of fiber. It is distinguished by its larger diameter core. Since there is so much space to move around inside, each pulse of light can travel a slightly different path to the other end of the fiber. This is called Multimode fiber, because there are multiple ways the light can bounce between the cladding as it transitions the length of the fiber. Multimode fiber is popular for use in LANs, with lower speed transmission requirements.
The three popular sizes of Multimode fiber are:
    62.5/125 um (micrometers/microns)
    50/125 um
    100/140 um
Single mode, represents the new generation of fibers, which involve a small inner core and provide less dispersion and distortion of the light signal. This provides a better transmission range and allows a greater distance between repeaters, 60 - 200 miles. Single-mode fiber is somewhat more expensive than Multimode alternatives and is designed for optimal lightwave propagation at 1350 and/or 1550 nm (nano meters) wavelengths. Laser diodes are primarily used with single mode systems.
The size of Single Mode fiber is:
    9/125 um

## Slide 26: Tipos de Fibra
Multimodo
Tipo Seção Perfil Largura de
Transversal Banda
Índice gradual
Monomodo
degrau
Índice degrau
1 2 5 10 20
GHz
(1 Kilometer)
Notes: <number>
<footer>
<header>
<date/time>
The three types of fiber most commonly used for fiber optic communications are:
    Multimode Step Index - This fiber is easy to manufacture, it typically has a large core and has a low bandwidth (10 MHz for 1 Km)
    Multimode Graded Index - This fiber is more difficult to manufacture because of the graded index profile. A carefully designed and manufactured core can yield very good bandwidths (1 to 2 GHz for 1 Km).
    Single Mode Step Index - This fiber requires a high degree of precision manufacturing because of the very small core dimensions. It produces very high bandwidths (30 to 50 GHz for 1 Km, depending on the optical source).

## Slide 27: Fibra Monomodo de Índice Degrau
Cladding
Core
Laser
Luz axial
perfil
Pulso
de
entrada
Pulso
de
saída
Notes: A single mode step-index fiber has a central core that is sufficiently small so that there is only one path that light may take as it propagates down the cable. Other modes entering the fiber are dissipated as cladding modes. The refractive index of the cladding is slightly less than that of the central core and is uniform throughout the cladding. This type of cable has a much higher critical angle, resulting is a small acceptance angle and a narrow source-to-fiber aperture. This makes it much more difficult to couple light into the fiber from a light source. With a very small fiber core, light will travel through the fiber along the axis of the core. This is know as light traveling along an axial path.
Advantages:
    Minimum dispersion
    Large bandwidth
  Disadvantages:
    Difficult to couple light into core
    more expensive
    laser source is required

## Slide 28: Fibra Multimodo de Índice Degrau
Luz Não Axial
(modos de alta ordem)
casca
núcleo
Pulso
de
entrada
Pulso
de saída
Perfil
Fonte
de luz
Notes: <number>
<footer>
<header>
<date/time>
With a larger core diameter in multimode, step index fiber, light waves will enter the core at different angles and will travel non-axially through the fiber (reflecting from the core cladding boundary). The non-axial waves will travel a greater distance than the axial wave, causing the light to arrive at the terminating point at different times. The is called modal dispersion.
Because the index of refraction of the core is constant throughout, the non-axial light rays travel in a straight path until they encounter the core/ cladding interface. If the angle of the ray at this interface does not exceed the critical angle of the fiber, the ray is reflected back toward the center of the core.
As the number of modes of light traversing the fiber increases, bandwidth tends to decrease. In addition to different pulses reaching the destination at slightly different, too much dispersion also results in light pulses overlapping and becoming undetectable by the receiver.
Advantages:
    Inexpensive and easy to manufacture
    easy to couple light into the fiber core
  Disadvantages:
    Limited bandwidth
    higher modal dispersion (signal spreading)

## Slide 29: Fibra Multimodo de Índice Degrau
Cladding
Core
Pulso
de
entrada
Pulso
de
saída
Perfil
Fonte
de luz
Notes: <number>
<footer>
<header>
<date/time>
A multimode graded-index fiber is characterized by a central core that has a refractive index that is not uniform; it is maximum at the center and decreases gradually toward the outer edge. Light is propagated down this type of fiber through refraction. Light enters the fiber at many different angles. As the light ray propagates down the fiber, the light rays that travel in the outermost area of the fiber travel a greater distance than the rays traveling near the center. The refractive index decreases with distance from the center and velocity is inversely proportional to the refractive index. This allows light rays traveling farthest from the center to propagate at a higher velocity. All the lightwaves take approximately the same amount of time to travel the length of the fiber.
Advantages:
    easier to couple light into and out of the fiber than single mode fiber.
    Distortion due to multiple propagation paths is less than multimode step-index fiber
    easier to manufacture than single mode
Disadvantages;
    more difficult to manufacture than multimode step-index
    considered an intermediate fiber

## Slide 30: Fibra de Índice Gradual
Casca
Index
Profile
Mudança do índice de refração em degraus, com
maior intensificação no eixo, faz com que a luz percorra um
trajeto sinuoso entre núcleo e casca e equaliza o retardo de
propagação
n
Notes: The index of refraction profile of a graded index fiber is actually a series of small step changes in the index of refraction (N) of the core material. The index (N) decreases slightly with each step from the core’s center towards the cladding.
As a light ray (mode) travels away from the center of the core, each change (decrease) in the index of refraction that it encounters causes it to refract or bend slightly back toward the core’s center.

## Slide 31: Comparação entre Fibras
Atenuação
Baixa
Menor
Mais alta
A menor
Largura
de banda
Moderada
Mais alta
Baixa
Muito
Alta
Abertura
Numérica
Média
Menor
A maior
Muito
Pequena
Diâmetro
Externo
125

m
125

m
140

m
125

m
Comp.
de onda
850 &
1300 nm
850 &
1300 nm
850 &
1300 nm
1300 &
1550 nm
62.5/125 50/125 100/140 Monomodo

## Slide 32: Perdas na Fibra
Fatores que contribuem:
    Espalhamento
    Absorção
    Micro and Macro curvaturas
Notes: Light is an electromagnetic wave of a vibrating (oscillating) nature. Just as the spped of light slows when traveling in transparent materials, each wavelength is transmitted differently in the fiber. Attenuation (optical power loss) must be measured in specific wavelengths for each fiber type. Losses of optical power at the different wavelengths occur in the fiber due to absorption, reflection, and scattering. These losses occur over distance depending on the specific fiber, fiber size, purity of the core, and the refractive index of the fiber.
Loss of light in fiber (attenuation) is caused by:
    Rayleigh scattering
    Scattering due to dopant oxide concentration fluctuations
    UV, IR, and OH absorption
      Ultraviolet Absorption
      Infrared Absorption
      Ion Resonance Absorption
    Microbending: effect where transmission loss increases due to fiber radius decreasing to the point where light rays begin to pass through the cladding boundary.
    Macrobending

## Slide 33: Espalhamento
Notes: Scattering (Rayleigh Backscatter) is the greatest source of loss in well made fiber. Light scattering is caused mainly by two mechanisms:
    The molecular structure of the glass material
    Inhomogeneities in the glass
During the manufacturing process, glass is extruded (drawn into long fibers of very small diameter). During the drawing process, the glass is in an elastic state (not liquid and not solid). The tension applied to the glass during this process causes the cooling glass to develop submicroscopic irregularities that are permanently formed in the fiber. When light rays propagating down the fiber strike one of these impurities, they are diffracted, causing the light to disperse or spread out in many directions. Some of the diffracted light continues down the fiber, some is reflected back toward the source, and some of it escapes through the cladding. The light rays that are reflected back toward the source and those that escape represent the loss in light power.
The light reflected back toward the light source (input to the fiber) is the property that is used in optical time domain reflectometers (OTDR) to measure loss at fiber joints and determine location of cable breaks.
Rayleigh Scattering loss = LRS = A / 4 ( = wavelength)
A  2 for Si O2 (Si O2 = silica oxide)

## Slide 34: Perda por Espalhamento vs Comprimento de onda
10
5
2
1
0.5
0.2
0.1
.05
.02
.08
1.0
1.2
1.4
1.6
Comprimento de onda (m)
Perda, dB/Km
Notes: The molecular structure of the glass is much smaller than the light’s wavelength (), and its relative size decreases as the light wavelength increases.
Because of this, as the wavelength () increases, the loss due to scattering decreases proportionally to 1/ 4

## Slide 35: Absorção
Notes: Absorption loss in optical fiber is analogous to power dissipation in copper cables. There are three factors that contribute to the absorption losses in optical cable, they are:
    Ultravilot absorption
    Ion resonance absorption
    Infrared absorption
Light energy is absorbed by the fiber as heat. Because fibers have such low loss, this amount of heat is extremely small and virtually undetectable.
In the early years of fiber manufacturing, it was difficult to keep water (OH) impurities in the fiber to a low level. Lightwaves at 1.25 micrometers (m) and 1.39 (m) cause molecular resonance of the OH ions, resulting in higher loss. Ion absorption is also caused by iron, copper, and chromium molecules.
Ultraviolet absorption is caused by valence electrons in the silica material from which fibers are manufactured. Light ionizes the valence electrons into conduction. The ionization is equivalent to a loss in the total light field and, contributes to the transmission losses of the fiber.
Infrared absorption is a result of photons of light that are absorbed by the atoms of the glass core molecules. The absorbed photons are converted to random mechanical vibrations typical of heating.

## Slide 36: Perda por Macrocurvatura
Macrocurvatura
Dano
Bolha de OH
Notes: Macrobending losses result from light scattering or deflection from the core due to small, abrupt changes in the core’s mechanical structure.
Sharp irregularities in the core/cladding interface caused during manufacturing, differences in thermal contraction rates between the core and cladding material, or by external forces result in macrobending losses. A macorbend represents a discontinuity in the fiber where Rayleigh scattering can occur. Stresses on the cable from hard rocks, tie wraps and clamps can also create this loss.

## Slide 37: Perda por Microcurvatura
Perda por
radiação
devido a
microcurvatura
Notes: Microbending (constant radius bending) occurs when the fiber bend radius decreases to the point where some of the light rays in the core begin to escape into the cladding. This causes the fiber rays to reflect at a different angle therefore creating a circumstance where the higher order modes are reflected into the cladding and escape. As the radius decreases, the attenuation increases due to this effect.
The radius at which this occurs depends on the type and size of the fiber and the wavelength of operation. Large core, multimode fibers are less sensitive (i.e., will tolerate a smaller bend radius) than single mode fibers.

## Slide 38: Dispersão
Dispersão Modal -Causada por diferenças nos tempos de propagação dos percursos de transmisssão (modes) ao longo da fibra (também chamada intermodal)
Dispersão Cromática -Causada pelo fato de que a velocidade de propagação da luz em uma fibra é diferente para diferentes comprimentos de onda e todas fonte ópticas produzem largura espectral finita (também chamada intramodal.
Notes: Dispersion is an effect where the optical modes (light rays) propagate down the fiber at different rates and arrive at the receiving end at different times. This has the effect of spreading the signal energy in time and reducing the amplitude of the pulse. Dispersion is measured in ps/nm/km (pico-seconds per nanometer per kilometer).
Multimode fibers exhibit both modal and chromatic dispersion. In systems using lasers as sources, chromatic dispersion is small and only modal dispersion needs to be considered. When LEDs are used, both modal and chromatic dispersion must be considered.
Single mode fibers exhibit only chromatic dispersion because they allow only one transmission mode. Chromatic dispersion consists of waveguide dispersion and material dispersion. Both are due to the optical source having a finite spectral width (light source wavelength).
  Waveguide dispersion is due to the geometry of the fiber which causes different wavelengths to propagate at different speeds.
  Material dispersion is caused by the glass material itself, which causes the propagation speed to vary with wavelength.

## Slide 39: Dispersão Modal
Input
Output
Notes: Modal dispersion, or pulse spreading, is caused by the difference in the propagation times of light rays that take different paths down a fiber. Light energy starting out as a short pulse at the input to the fiber is spread out, or “dispersed” over time as it propagates down the fiber. Modal dispersion only occurs in multimode fibers.
  Dispersion causes broadening of the electrical pulses in the receiver. How much broadening takes place is a function of how much dispersion there is in the fiber and fiber length.
  At low data rates, this does not cause a problem, because the pulse broadening or spreading is small compared to the data pulse width.
  At higher data rates, adjacent pulses begin to interfere with each other. (intersymbol interference). This can cause data errors in the receiver.
Modal dispersion can be reduced by using graded-index fibers and almost entirely eliminated using single mode fibers.

## Slide 40: Dispersão em Fibra com Índice Degrau
c
Percurso mais
curto
(modo fundamental)
L / sin1
Percurso mais longo
Modo de mais alta ordem
L
Notes: In a multimode fiber, light energy starting out at the same instant in time travels down the fiber over a large number of paths (modes). Although light travels down each path at the same velocity, the paths have different lengths, with the fundamental mode having the shortest length. This causes the light energy to arrive at the other end at different times.
In 1 kilometer of step index fiber, it can be shown using simple geometry that there can be as much as 15 meters difference between mode path lengths.
    If the index of refraction of the fiber core is 1.48, the speed of light in the fiber is:
    c/n = 3 x 108m/sec = 2.03 x 108m/sec
    1.48
    Therefore, the difference in propagation time is:
     t = 14m  2.03 x 108m/sec = 69 nanosec

## Slide 41: Dispersão Cromática
LED
Luz axial
Perfil do
índice
Notes: The refractive index of a material is wavelength dependent. Light-emitting diodes (LEDs) emit light that contains a combination of wavelengths. Each wavelength within the composite light signal travels at a different velocity. Light rays that are simultaneously emitted from an LED and propagate down an optical fiber do not arrive at the far end of the fiber at the same time. This results in a distorted receive signal and is called chromatic distortion. Chromatic distortion can be eliminated by using a monochromatic source such as an injection laser diode (ILD).

## Slide 42: Tipos de Fibras
Casca
Plástica
Núcleo
Plástico
Casca
Plástica
Núcleo
Vítreo
Núcleo
vítreo
Casca de
Vidro
Notes: There are three varieties of optical fibers available today. All three varieties are constructed of either glass, plastic, or a combination of glass and plastic.
    Plastic core and cladding
    Glass core with plastic cladding (referred to as PCS fiber, plastic clad silica)
    Glass core and cladding (referred to as SCS, silica clad silica)
Plastic fibers have several advantages over glass. They are more flexible and more rugged than glass. They are easyier to install, can better withstand stress, are less expensive, and weigh approximately 60% less than glass. The disadvantage of is their high attenuation characteristic; they do not propagate light as efficiently as glass. Plastic fibers are limited to relatively short runs, such as within a single building, or a building complex. Modern technology is improving the quality of plastic fibers and they are becoming more efficient.
Fibers with glass cores exhibit low attenuation characteristics. PCS fibers are slightly better than SCS fibers and are less affected by radiation. SCS fibers have the best propagation characteristics and are easier to terminate than PCS fibers. SCS fiber cables are the least rugged and are more susceptible to increases in attenuation when exposed to radiation.

## Slide 43: Construção do cabo
Estrutura Loose
Tubo de proteção
Fibra com
revestimento
secundário
Polyurethane
Kevlar
Hytrel Secondary Buffer
Fibra
Silastic Primary Buffer
Polietileno
Revestimento de alumínio corrugado
Mylar Tape Wrap
Polyurethane
Agrupamento de fibras
Núcleo rígido (plástico ou aço)
Polyurethane
Elementos de tração
Thermal Wrap
Polyurethane Tube
Fiber Ribbons
Estrutura tight (aderente)
“Multiple Strands”
Cabo telefônico
Notes: There are many different designs available today. Several different examples of several fiber optic cable configurations are show above. Depending on the configuration, the cable may include a core, a cladding, a protective tube, buffers, strength members, and one or more protective jackets.
With the loose tube construction, each fiber is contained in a pretective tube. Inside the protective tube, a polyurethane compound encapsulates the fiber and prevents moisture from entering the tube.
To increase the tensile strength of the multiple-strand configuration, a steel or plastic central member and a layer of Mylar tape wrap are included in the construction. The encapsulated ribbon cable is most often seen in telephone systems that use fiber optics.
The type of construction used depends on the performance requirements of the systems and both the economic and environmental constraints.

## Slide 44: Atenuação
100% 79.4% 63.1% 50.1% 31.4% 20%
-7 dB
-2 dB
-3 dB
-5 dB
-1 dB
Distância
Potência Relativa
Nível do sinal ao longo da fibra
Expressa como dB/km, atenuação é perda de luz ou de potência do sinal
0 dB
Notes: When using an optical fiber, attenuation is dependent upon the operating wavelength; the greater the wavelength the lower the attenuation.
Attenuation in optical fibers can be identified as intrinsic or extrinsic:
    Intrinsic Loss
      Absorption
      Scattering
      Fiber Core Variations
      Macrobends
    Extrinsic Loss
      Connectors
      Couplers
      Attenuatiors
      Splices
      End Finishes
      Microbends
    Intrinsic/Extrinsic
      Fiber Core and Numerical Aperture Mismatch

## Slide 45: Perda por Reflexão de Fresnel
Reflexão de Fresnel na Interface
n1
n2
Núcleo da fibra
Reflexão dupla numa junção
Notes: Fresnel reflection is the change in direction of a light beam at an interface between tow dissimilar media so that the light beam returns into the medium from which it originated.
  Fresnel reflection occurs at the air-glass interfaces at entrance and exit ends of an optical waveguide. Resultant transmission losses (on the order of 4% per interface) can be virtually eliminated by the use of antireflection coatings or index matching materials.
  Fresnel reflection depends upon the index difference and the angle of incidence. In optical elements, a thin transparent film is sometimes used to give an additional Fresnel reflection that cancels the original one by interference. This is called an antireflection coating.
To avoid unnecessary loss of light, the input and exit surfaces of an optical fiber must be smooth and perpendicular to the axis. Even with optically flat ends, a small proportion of the incident light is reflected back, this being an unavoidable phenomenon associated with a step change in refractive index. The magnitude of this reflection is about 4% for a typical air-glass interface, and is the same whether light is entering or leaving the fiber. Consequently, a fiber-to-fiber coupling, involving two interfaces, introduces a total loss of nearly 8%, or about 0.35 dB.

## Slide 46: Redução de Perdas de Fresnel
Líquido casador de índice n  nc
nc
nc
Utiliza-se casamento de índice de refração
Notes: Fresnel reflection can be reduced to a very low level by filling the gap between adjacent fibers ends with an index matching liquid. This is a liquid that exhibits the same refractive index as the fiber core.
Index matching is not considered to be a practical approach in demountable connectors since direct collection is a major problem with such liquids. It is very successful in reducing loss in the more permanent mechanical splice joints.